## Slide 1: High-purity Water Recovery from Produced Water via Membrane Distillation
2nd Annual State of the Science Symposium
Jianjia Yu
Assistant Professor of Chemical Engineering Research Engineer/Section Head
Petroleum Recovery Research Center (PRRC)
New Mexico Institute of Mining and Technology, Socorro, NM 87801
August 26, 2025

## Slide 2: Where is the PRRC?
Located in Socorro;
Central location ~3-4 hour drive to all producing areas in the state.

## Slide 3: GO-TECH
New Mexico Water and Infrastructure Data System (NM WAIDS), Led by Martha Cather.
GO-TECH Web Site (production data, well info, produced water data, etc).
>10 million page views each year!
Water quality data available for
~9,400 wells and volume data for over 75,000 wells on GO-TECH.
(From Martha Cather, 2025)

## Slide 4: Produced Water Treatment at PRRC/NMT
1998
2013
2016
2018
2009
2021
2023
(1998 - current)

## Slide 5: Objective: to develop novel, portable, and scalable robust hollow fiber membrane-based separation processes that convert produced water into a sustainable water resource.
Organics removal
Ultrafiltration
Microfiltration
Membrane adsorption
Hybrid processes
Desalination/ Resource Recovery
Nanofiltration
Reverse/Forward osmosis
Membrane distillation
Hybrid processes
Hollow fiber membranes
Compared to flat sheet membrane:
higher productivity per unit volume (high packing density and large surface area)
For a 0.04 m3 membrane device:
HF membrane: 575 m2 (90 mm in diameter);
Spiral wound fiat-sheet membrane: 30 m2;
Tubular configuration: 5 m2.
self-supporting
small footprint, easy to scalable
Hollow fiber membrane module*
* https://www.permselect.com/membranes

## Slide 6: Direct Contact Membrane Distillation (DCMD)
Very few full-scale MD tests have been reported in the world.
Main challenges: (1) lack of commercially available membranes for particular use in DCMD; (2) energy consumption.

## Slide 7: Hollow fiber membranes
Properties of the fabricated Janus hollow fiber membrane.
(μm) | (ε, %) | porosity (εe, m-1) | (da, μm) | (dm, μm) | (bar)
1088/767/135 | 80.6±0.4 | 6471.3 | 0.27 | 0.40 | 1.95
OD/ID/WT
Bulk Porosity Mean pore size
Effective surface Bubble point pore size LEP

## Slide 9: DCMD Process for PW Desalination
Apparatus of hollow fiber membrane-based DCMD process for high-salinity brines desalination.
Membrane modules assembled for the DCMD experiments.

## Slide 10: Desalination Performance Evaluation
Salt rejection: >99.9%

## Slide 11: Long-term desalination performance evaluation
0
20
40
60
0
10
20
30
40
50
80 100 120 140 160 180 200
Time (hr)
Water Flux (kg/m2h)
0
5
10
15
20
25
30
35
40
Conductivity (S/cm)
SW: TDS=35,000 mg/L
Operating conditions:
T-feed: 60°C;
T-permeate: 20°C;
ν-feed: 0.8 m/s
ν -permeate: 0.6 m/s
No significant scaling and wetting during a continuous 200 hours of DCMD operation.
Typical drinking water: 50 - 500 µS/cm (25 °C).

## Slide 12
PW: TDS=155,000 mg/L NPOC=57.6 mg/L
Operating conditions:
T-Feed: 60°C;
T-Permeate: 20°C;
ν-feed: 0.4 m/s
ν -permeate: 0.4 m/s
Due to the complicate composition of PW, membrane regeneration was preformed for 30 mins every 12 hours.
No membrane wetting, the salt rejection remains higher than 99.99%.
Water samples: (a) actual oilfield produced water; (b) pre-treated with a 50 µm filter;
(c) product water.

## Slide 13: Tech-economic analysis
- Assumptions:
Plant capacity: 500,000 GPD;
Plant lifetime: 30 Years;
Plant availability: 90%; 100,000 mg/L
PW - initial TDS:;
PW – concentrated brine: 200,000 mg/L;
PW - recovered: <500 ppm;
Water recovery: 50%;
Membrane cost: $20/m2;
Membrane replacement: 20%/year;
Pretreatment: $80/m3/day;
Electricity cost: $0.069/kwh;
Steam price: $0.008/kg

## Slide 14
Base case
With heat integration
0.0
0.2
0.4
0.6
0.8
1.0
Cost ($/bbl.)
O&M cost
Capital cost
transportation/intake of PW to the DCMD system.
The cost does not include the transportation/disposal of the brine concentrate.
The recovery factor is 50%.
$0.87
The cost does not include the
$0.10

## Slide 15
DOE list of the most important critical materials with respect to energy and supply chain risk.

## Slide 16
https://www.energy.gov/fecm/articles/doe-invests-additional-8-million- increase-domestic-supplies-water-and-critical

## Slide 17: Acknowledgement